THESIS INFORMATION

Thesis title: “Research and fabricate SERS substrates based on materials of Ag nanoparticles, ZnO, Al2O3 for detect pharmaceutical substances”

Speciality: Optics

Code: 9440110

Name of PhD Student: Le Thi Minh Huyen

Academic year: 2019

Supervisor: Assoc. Prof. PhD. Le Vu Tuan Hung

At: VNUHCM - University of Science

1. SUMMARY:

This thesis investigates the conditions for fabricating the Surface-enhanced Raman scattering substrates (SERS) based on materials of Ag nanoparticles, ZnO, Al2O3 to improve the performance of SERS substrates. The fabrication process and characteristics of Ag nanoparticles, Al2O3 doped ZnO nanofilms (AZO), and ZnO/Al/a-Al2O3 nanorods are established. In addition, this research has developed a method for analyzing the reagent rhodamine 6G (R6G), the pharmaceutical substances ketoprofen (KP) and metronidazole (MNZ), based on the fabricated SERS substrates, according to ICH guideline Q2(R2) on validation of analytical procedures.

2. NOVELTY OF THESIS:

- The AZO/Ag nanofilm SERS substrate fabricated in this thesis is a new generation SERS substrate. Ag nanoparticles have a spherical shape with an average size of about 30–40 nm attached to the AZO nanofilm (consisting of 98 wt% ZnO doped with 2 wt% Al2O3). The AZO film is coated on a flat glass slide by DC magnetron sputtering method with optimal fabrication parameters at a sputtering time of 45 min. The performance of the AZO/Ag SERS substrate was significantly improved due to detect the R6G reagent at limit of detection (LOD) ~ 10–9 ppm with SERS substrate enhancement factor (SSEF) ~ 2.0  1015. The AZO/Ag nanofilm SERS substrate detected the KP and MNZ drug standards at LOD of 5   10–2 ppm and 5  10–3 ppm, respectively.

- The ZnO/Al/a-Al2O3/Ag nanorods SERS substrate fabricated in the thesis is a new generation SERS substrate. The spherical Ag nanoparticles with an average size of about 20 nm and evenly distributed on the ZnO/Al/a-Al2O3 nanorods. ZnO/Al/a-Al2O3 nanorods are synthesized by sol-gel method, chemical bath deposition and vacuum thermal evaporation method under optimal conditions with 1.0 mg Al. The ZnO/Al/a-Al2O3/Ag SERS substrate performance is improved due to detect the reagent R6G at LOD ~ 10–5 ppm with SSEF ~ 1.9  1010. ZnO/Al/a-Al2O3/Ag nanorods SERS substrate detected the KP and MNZ standard solutions at LOD of 5  10–1 ppm and 10–2 ppm, respectively.

- Propose the charge transfer diagram between the SERS substrates of AZO/Ag nanofilm, ZnO/Al/a-Al2O3/Ag nanorods and R6G, KP, MNZ molecules to explain the improvement in sensitivity of SERS substrates in the thesis.

- The analytical method based on SERS substrates in this thesis is used to determine the pharmaceutical substances KP and MNZ according to ICH guidelines Q2(R2) as a qualitative and semi-quantitative method. This method for detecting KP and MNZ has specificity and low detection limit. The method using AZO/Ag nanofilm and ZnO/Al/a-Al2O3/Ag nanorods SERS substrates responses the linearity requirement and is promising to be used for quantitative analysis of MNZ. The spectral reproducibility of the method, evaluated through R6G reagent, has good spectral repeatability with RSD < 15% in all measured samples and satisfies independent verification through ANOVA analysis.

3. APPLICATIONS/ APPLICABILITY/ PERSPECTIVE

- The SERS technique based on AZO/Ag nanofilm substrates and ZnO/Al/a-Al2O3/Ag nanorods can be applied to quickly detect pharmaceutical substances or toxic chemical residues in food, to ensure health for consumers.

- Investigation of sample preparation methods to improve the repeatability of drug analysis methods based on the AZO/Ag and ZnO/Al/a-Al2O3/Ag nanorods SERS substrates.

- Improve the SERS substrate fabrication techniques and sample measurement methods to develop new low-cost and effective analysis methods.

| SUPERVISOR | PhD STUDENT |
| --- | --- |

CONFIRMATION UNIVERSITY OF SCIENCE

PRESIDENT