# THESIS INFORMATION

Thesis title:	 "Synthesis and functionalization of acidic metal-organic frameworks for catalysis and adsorption"

Speciality: 	Organic Chemistry

Code: 	9440114

Name of PhD Student:	Nguyen Ho Thuy Linh

Academic year:	K29/2019

Supervisors: 	1. Assoc. Prof. PhD. Tran Hoang Phuong

2. PhD. Doan Le Hoang Tan

At: VNUHCM - University of Science

1. SUMMARY

- Objective and methodology

- Zr-MOF and Hf-MOF materials with 6- and 12-coordinated were synthesized  via solvothermal method and microwave irradiation to generate materials containing defects and Lewis/Brønsted acid sites. In addition, cluster functionalization was applied to incorporate the Brønsted acid group on the 6-coordinated Hf-MOF.

- PXRD, TGA, FT-IR, N2 sorption, and SEM were applied to characterize the MOFs’ structure and properties for the explaination of relationship between their structure, strength, and activity.

- The catalytic activity of MOF were studied in the addition and cyclization reactions to synthesize quinazolinone and benzoxazole. The sulfuric-functionalized Hf-MOF material was used as an efficient catalyst in the dehydration reaction for the synthesis of 5-HMF.

- The adsorption conditions for organic dyes such as methylene blue (MB), methyl orange (MO), and some other compounds such as indole and fluoride were investigated.

- Experimental procedure

- In the thesis, the structure and properties and materials were analyzed by methods such as powder X-ray diffraction (PXRD), Bruker D8 Advance; infrared spectroscopy (FT-IR), Bruker Vertex 70; differential thermal gravimetric (TGA), TA Q500 Thermal Analysis System; 77K nitrogen gas adsorption, Quantachrome Autosorb-iQ2; scanning electron microscope (SEM), Hitachi TM3000; and acid-base titration (Metter Toledo).

- In addition, gas chromatography (GC) methods coupled with mass spectrometry (MS), and flame ionization (FID) detectors, Agilent 5977N, and a capillary DB–5MS column (30 m x 250 µm x 0.25 µm); ultraviolet-visible spectroscopy (UV-VIS), JASCO V-670 spectrophotometer; High performance liquid chromatography (HPLC), HPLC Agilent technologies 126 infinity system are used for compositional analysis and product quantification in catalytic and adsorption applications studies.

- Results and conclusions

- The thesis results have synthesized and analyzed the structure and properties of Zr-MOF and Hf-MOF groups with 6 and 12-coordinated. Among them, Zr-BDC and Zr-NDC (12-coordinated) were synthesized by microwave method and showed an increase in surface area and pore size compared with materials synthesized by solvothermal method.

- In quinazolinone synthesis, Zr-BDC-MW has higher catalytic ability than Zr-BDC-ST and some other traditional acid catalysts thanks to the increase in the catalytic activity sites and pore space. With the help of microwave irradiation and without the use of solvents, the 6-coordinated Hf-based MOF catalyzes more efficiently than the 12-coordinated Zr-based MOF and can shorten the synthesis time while maintaining efficiency. The reaction of converting glucose to 5-HMF on Hf-BTC-SO4 material shows the supporting role of ionic liquid and acid-catalyzed sites of MOF in the isomerization and dehydration steps.

- 12-coordinated MOFs including Zr-BDC, Hf-BDC, and Zr-NDC were studied for indole, methyl blue, and methyl orange adsorption. Among them, Zr-BDC and Hf-BDC adsorb indole with adsoption capacity over 150 m2 g-1 and loading efficiency over 80%. The loaded indole into MOF showed an effective capture of fluoride ions at a concentration of 1000 ppm after 120 min and could be monitored through the fluorescence on/off mechanism. The study shows the potential of IND@MOF in fabricating sensors that capture fluoride ions in water and biological environments. The Zr-NDC material synthesized by microwave method can absorb MB and MO reaching 746.30 and 725.95 mg g-1 higher than this material synthesized at the solvent heat condition of 585.45 and 537.80 mg g-1. The acidic properties and stability of this MOF determine the effective adsorption capacity of the material in the pH range of 2-7 and give it the ability to be reused more than 5 times without significantly affecting the adsorption performance. Research results show that Zr-NDC materials are very potential to be used as adsorbents for environmental remediation.

2. NOVELTY OF THESIS

- Research on synthesis and characterization of Zr-BDC and Zr-NDC materials by solvothermal and microwave methods.

- The investigation on the catalytic ability of some 6- and 12-coordinated Zr-MOF and Hf-MOF materials in synthesizing quinazolinone framework compounds between anthramide and ketone under traditional heat and microwave irradiation conditions. Or the combination of  Hf-BTC-SO4 and ionic liquid solvent in the glucose/fructose conversion reaction to 5-HMF.

- Study of adsorption of organic dyes or indole on 12-connected MOFs towards environmental and biomedical applications.

3. APPLICATIONS/ APPLICABILITY/ PERSPECTIVE

- The results of the thesis are obtained from the interdisciplinary research of Materials - Chemistry - Environment.

- The reaction to convert glucose into 5-HMF under catalysis of MOFs in ionic liquid solvents can be applied to increase biomass conversion efficiency in synthesis of feedstock for the production of fuels.

- Research on fluoride sensing materials from durable MOF materials can must be developed to increase detection at low concentrations and applications in environmental remediation and biomedicine.